## Slide 1: Light-Emitting Diodes (LED)
Lecturer: Mauro Mosca
(www.dieet.unipa.it/tfl)
last release: 02/11/2020
University of Palermo – Master in Electronic Engineering

## Slide 2: LED: injection luminescence
p
n
EC
EV
EF
EF
p
n
V0
EC - EV = hc/l

## Slide 3: LED: radiative recombination
bimolecular recombination equation
In order to have a high radiative recombination…
… it is necessary that junctions are high-doped

## Slide 4: LED: radiative recombination
by excitons

## Slide 5: LED:
radiative recombination
NON

## Slide 6: LED: non-radiative recombination
deep-level
Auger
radiant process predominant
at low temperature

## Slide 7: Emission linewidths
density of states
N(E), Z(E)
effective mass

## Slide 8: Emission linewidths
Dn = 1.8 kT/h

## Slide 9: LED construction
n+-p diode
less self-absorption
recombination close to the junction
opaque substrate

## Slide 10: Light extraction
total internal reflection
qc = arcsin(n2/n1)
n1sinq1 = n2sin(90°)
most rays strike the surface at an angle less than the critical angle
ENCAPSULATION
TECHNIQUE
nepoxy (≈1.5) > nair
n1 – nepoxy < n1 - nair
Fepoxy > Fair
losses epoxy/air interface
minimized by moulding the epoxy into an hemispherical shape

## Slide 11: Exercise
Calculate the fraction of light transmitted by isotropic radiation F originated from a GaAs LED. Perform the same calculation for a LED encapsulated in an epoxy resin with an index of 1.5.
For the GaAs, consider n = 3.6
Solution:
F = 0.013 (1,3%) for GaAs/air
F = 0.036 (3,6%) for GaAs/epoxy/air

## Slide 12
Radiation pattern
0.5

## Slide 13: Electrical properties
diffusion voltage (or built-in voltage, or potential barrier)

## Slide 14: Electrical properties
Eg

## Slide 15: Electrical properties
nitride-based LEDs
AlGaInP-based LEDs

## Slide 16: Electrical properties

## Slide 17: Light-current characteristic

## Slide 18: LED drive circuit for d.c. operations
+
Vd

## Slide 19: LED drive circuit for a.c. operations

## Slide 20: LED on/off modulation circuit

## Slide 21: LED linear modulation circuit

## Slide 22: Efficiency

## Slide 23: Difficult to obtain high efficiency?
large active region (minority carriers limited
only by diffusion)
radiative recombination speed proportional to
carrier concentration: R = Bnp
(if the active region is large, the concentration –
that is, the number of charges per unit of volume –
is small)
non-localized carriers (unless…)

## Slide 24: Double heterostructure
(a)
(b)
charges confined within the
narrowest bandgap region
HOMOJUNCTION
HETEROJUNCTION
charges distributed over a distance
equal to the diffusion length

## Slide 25: Quantum-well
DOUBLE HETEROSTRUCTURE
QUANTUM-WELL STRUCTURE
localization increases
self-absorption decreases
(thin active region)

## Slide 26: Separate Confinement Heterostructures (SCHs)
In a double heterostructure, the narrower bandgap region usually also has a higher refractive index
even photons are confined !!
confined charges
confined photons
Separate Confinement
Heterostructure (SCH)
GRaded INdex Separate Confinement
Heterostructure (GRINSCH)
improves the overlap between the optical wave
and quantum well regions

## Slide 27: Carrier Loss
Analogy of the bucket of water...
too much water and the bucket overflows!
saturation of the
optical intensity
high current
injection
To limit overflow, the current injection areas can be sized
so that they have large areas, which means large electrical contacts

## Slide 28: Carrier loss
Optical intensity emitted by an LED in In0.16Ga0.84As/GaAs with active regions consisting of 1, 4, 6 and 8 quantum wells and theoretical intensity of a perfect isotropic emitter (in dashed line)
carrier
overflow
Using a large number of QWs, the overflow is more limited

## Slide 29: Electron-blocking layer
undoped structure
doped structure
no barrier to the
flow of holes

## Slide 30: Light extraction: light escape cone
ηextr ≈ γrefl
problem of re-absorption
problem of the internal reflection at the interface semiconductor–air.
shadowing of the emission by the top contact
absorption factor
reflection factor
shadowing factor

## Slide 31: Light extraction: light escape cone
For θint ≤ θc
TE (s) polarization:
(θi = 0)
for isotropic emission and R ~ R0

## Slide 32: Light extraction: light escape cone
Tab. 1 – Extraction properties for interface GaAs–air at 650 and 970 nm
Tab. 2 – Extraction properties for interface GaAs–epoxy at 650 and 970 nm
critical angle higher in the presence of epoxy (lower index difference)
high epoxy-air critical angle (epoxy index close to that of the air)
the epoxy can be modeled in the shape of a hemisphere so that the light rays coming from the center are practically perpendicular to the surface of the epoxy

## Slide 33: Optimization Standard Geometry
Light extraction cones for different LED geometries (based on standard rectangular
base parallelepiped geometry):
(a) absorbing substrate with with thin window layer
(b) absorbing substrate with thick window layer
(c) transparent substrate with thick window layer
active region close to the surface
absorbing
substrate
efficiency increases by a factor of
?
3
efficiency increases by a factor of 6

## Slide 34: Optimization Standard Geometry
Extraction efficiency increasing through
thick upper window and transparent substrate
Cross-section schematics of ideal geometries; sphere with
point source (left), hemisphere (middle) and a truncated cone (right)
 = ( /2 – c) / 2

## Slide 35: Techniques to fabricate high-efficiency LEDs
Evolution of external quantum efficiency improvements for LEDs in AlGaInP
(hext calculated considering the LED immersed in an epoxy dome)
Year | Design | hext (%)
1990 | DH on GaAs substrate (standard LED) | ≈ 2
1992 | thick GaP window layer | ≥ 6
1994 | transparent GaP substrate | 17,6
1996 | idem | 23,7
1999 | idem + MQW | 32,0

## Slide 36: Techniques to fabricate high-efficiency LEDs
Two different generations of amber AlGaInP LEDs by Hewlett-Packard (now Lumileds):
- absorbing GaAs substrate (AS) LED with thick GaP window layer
- wafer-bonded transparent GaP substrate (TS) LED
wafer
bonding
etching
chimico

## Slide 37: Techniques to fabricate high-efficiency LEDs: TIP geometries
TIP geometry devices: (a) InGaN blue LEDs on SiC substrate, marketed under the name “Aton”; (b) Diagram of the path of the rays in the LED
(c) AlGaInP / GaP LEDs; (d) Diagram of the path of the rays in the LED
h = 55%

## Slide 38: Techniques to fabricate high-efficiency LEDs: Thin-film LEDs
a) LEDs with reflecting mirror
b) Surface-Textured LEDs
bonded on a gold-coated dielectric mirror
epitaxial lift-off
high etching selectivity of AlGaAs alloys in hydrofluoric acid
h = 72%
photon recycling
GaN etching
natural lithography

## Slide 39: Techniques to fabricate high-efficiency LEDs: Thin-film LEDs
c) Buried micro-reflector LEDs
(BMR LEDs)
d) Tapered LEDs
must be

## Slide 40: Tapered LEDs: photoresist reflow
(a)
(b)